Mu-copper faraday cages钼铜法拉第箱子-钼铜墙纸

We produce Faraday cages, shielded chambers and other shielding components like我们生产法拉第箱子，屏蔽室和其它的屏蔽部件，如:

- Power & signal filters电源和信号线滤波器 (see webpage)

- Waveguides for data communication 用于数据通信的波导

- shielded doors屏蔽门 (see webpage)

- Windows窗户 (see webpage)

- Shielded ventilation panels屏蔽通风板 (see webpage).

In addition we produce, TEMPEST equipment for crypto communication and even welded EMP bunkers. We have a large standard range in stock and we can deliver to the cage building industry in mere days. We also design items according to the client’s wishes, with very short delivery times.

另外我们生产TEMPEST防信息泄漏设备用于保密机通信和即使是焊接的EMP箱体。

Wall covering system (Mu-copper)墙面材料系统（钼-铜墙纸）

Mu-Copper foil has high attenuation properties in the electrical field (up to 120 dB) as well as in the magnetic field (see shielding performance table).

钼铜薄片在电场（可达120 dB）以及磁场方面有高的衰减特性（看屏蔽性能表）

It is easy to apply, like wallpaper, thanks to its special adhesive for walls, ceilings and floors. The interior finish can be plaster board, foam tiles or plywood.

它是容易使用的，像墙纸，由于它的特殊黏合剂，用于墙、顶棚和地面。室内装修能是糊墙纸板，泡沫瓦片或胶合板。

The 0.12 mm thick Mu-Copper is used to transform regular rooms into shielded rooms; it has excellent shielding performance even at low frequencies. The system is easy to mount on shielded doors with clamping devices. The standard width of Mu-Copper is 1000 mm and the foil can be delivered on rolls or ready-made sheets.

0.12mm厚的钼铜被用于改变正常的房间成为屏蔽室，它有极好的屏蔽性能即使在低频。该系统用夹具是容易装配在屏蔽门上的。钼铜的标准宽度是1000mm，薄片的交货可以是卷状的或是预先做好的薄片。

Overlap options重叠选择

For the joints you can use a 50 mm overlap. For extra high performance you can fully solder the joint or use a seaming /copper tape with a conductive self-adhesive to apply over the joints.

对于接合处你能使用一个50mm的重叠部分。对于特别要求的高性能你可以完全的焊接结合点或使用一个带有自粘的接缝/铜带以应用在接缝点上。

Advantages优势

- Cost-effective / takes up little space 物有所值/占据很小的空间

- Light weight / high floor load 轻重量/高地板载重

- Can be constructed with local labor 能用本地的劳工建造

- Standard interior finish possible like plasterboard 标准的室内装修很像石膏板

- Can be delivered with 10 year guarantee 10年的保质期

- Maintenance free 维护方便

- Delivery with turnkey measurement report 交货时带有测量报告

Shielding performance屏蔽性能

Basic values for the material and Mu-copper cage 用于材料和钼铜箱子的基值

| Field场 | Frequency频率 | Mu-copper钼铜 |
| --- | --- | --- |
| H | 1 kHz | 22 dB |
| H | 10 kHz | 33 dB |
| H | 200 kHz | 68 dB |
| E | 10 kHz | 99 dB |
| E | 200 kHz | 127 dB |
| E | 1 MHz | 125 dB |
| E | 18 MHz | 101 dB |
| P | 400 MHz | 120 dB |
| P | 1 GHz | 110 dB |
| P | 10 GHz | 120 dB |
| Shielding performance of mu-copper foil 0.12 mm thick |

Measurements according to MIL STD 285 and the following situation:测量依据MIL STD 285和下列的情形：

- Mu-copper foil 0.12 mm thick fully soldered 钼铜薄片0.12mm厚完全焊接

- Dimensions尺寸 10 x 6 x 4 m

- 1 Door门 0.9 x 2.1 m

- 2 Ventilation panels 通风板

- 4 Power filters电源滤波器

You can create a Faraday cage with high shielding performance yourself in an economic way, using local labor. This is possible in existing buildings as well as in new ones, without loss of space. Depending on the quality of the doors, vent panels, filters and/or windows used, attenuation levels up to 80-100 dB in the E-field can be realized. When more layers are applied, it is possible to achieve over 120 dB.

你能自己用一个经济的方法建造一个法拉第箱子，使用本地的劳工。这个可以用在现有的建筑以及新的建筑，没有损失空间。依据使用的门、通风板、滤波器和/或窗户的质量，可以实现在E场的衰减级别可达80-100 dB。当使用多层时，它可以实现在120 dB以上。

Ventilation通风设备

For ventilation we have developed honeycomb ventilation panels. Special for the mu copper faraday cages we can deliver honeycomb vent panels with a mu copper flap arround. Can be easily soldered into the mu copper faracay cage.

对于通风设备我们已经开发了蜂窝通风板。特别对于钼铜法拉第箱子我们能交付蜂窝通风板带有一个钼铜围边。能很容易地焊接到钼铜法拉第箱子。

For other honeycomb ventilation panels see our honeycomb ventilation webpage.对于其它的蜂窝通风板，看我们的蜂窝通风设备网站。

Ceiling顶棚

The system can be used with a detachable or fixed ceiling to separate existing ducts and cables from the shielded room.

该系统能被使用为一个可分开的或不变的顶棚以隔离来自屏蔽室的现有的管道和电缆。

Detachable ceiling construction可拆开的顶棚结构

| Applications应用 Server rooms 服务器室 EMC test rooms 电磁兼容测试室 Computer rooms 计算机室 Medical examination rooms 医学检查室 MRI, EEG, EMG & EVP Rooms for physiotherapy 理疗室 Radar protection/Airport 雷达保护/机场 TEMPEST Sites 防信息泄漏场所 Military EMC protection 军用EMC保护 Board room shielding 会议室屏蔽 Industrial espionage/ Secure room 工业间谍/保密室 Buildings for intelligence agencies 情报部门的建筑 For more information download datasheet "Medical solutions" | Server rooms服务器室 MRI rooms 核磁共振室 |
| --- | --- |

| Modified RF Shielded Door 改进RF屏蔽门 When a lower performance 40-60 dB is acceptable we can retrofit your existing door. The doors will be equipped with gaskets on top and sides, while the bottom is provided with a conductive copper brush and doorstep. 当一个较低性能40-60dB是可接受的，我们能翻新你的现有的门。门在顶部和侧边装备垫圈，同时在底部装备一个导电的铜刷和门阶。 Modification is possible for both swing and sliding doors. 对于旋转门和滑动门两种都可能进行改进。 For heavy duty applicaations we deliver faraday cage doors up to 140 dB reduction. 对于一些重载的应用，我们交付法拉第箱子门可达140 dB减少量。 For more information see our faraday cage doors webpage | Shielding sliding door屏蔽滑动门 |
| --- | --- |

Components部件

In addition to EM shielded doors and windows, the screened rooms can be equipped with the following components:除了EM电磁屏蔽门和窗以外，屏蔽室能用下列部件装备：

- Shielded doors (see webpage) 屏蔽门

- Shielded windows (see webpage) 屏蔽窗

- Shielded ventilation panels (see webpage) 屏蔽通风板

- Power and signal filters (see webpage) 电源和信号滤波器

When necessary we also offer shielding solutions for water pipes, medical gases and ventilation.

当需要时，对于水管、医疗气体和通风我们也提供屏蔽解决。

Example pictures图例

Click to enlarge image

Project: University Amsterdam test labaratory

Project: Animal hospital Belgium, Horse MRI room