Conductive Tapes 3200导电带

A large series of tapes, which are electrically conductive. 一个大系列的导电带。

Ideal for earthing, conductance and EMI shielding. 理想的用于接地，电导和EMI屏蔽。

Metal Tape with conductive self-adhesive带有导电自粘的金属带

Electrically conductive tapes can be cut to any width from 3 mm wide and can be delivered from stock. A width of 25 mm is used most commonly. Standard roll length 16.5 meters.

导电带能被剪切成从3mm宽开始的任何宽度，能从现库存交货。一个宽度为25mm的带子是最通用的。标准卷长度是16.5米。

When you need to cover bigger surfaces you can contact our engineers because than you can possible better use this tape in combination with copper foil with a non-conductive adhesive. This is a much cheaper solution.

当你需要覆盖更大的表面时你可以联系我们的工程师因为比你可能更好的使用这个带子在使用一个非导电的自粘使铜带子结合。这是一个更便宜的解决。

Applications应用

- Electrical connection between surfaces (sheets / foils) 在表面之间的电连接(薄片/箔)

- Die-cuts 冲切

- Mounting transparent foils, windows 安装透明薄片，窗户

- Shielding in housings 机壳里屏蔽

- Cable shielding 电缆屏蔽

- Temporary shielding during tests 在测试期间临时屏蔽

- Antistatic floor 抗静电地板

Shielding effectiveness屏蔽效能

Many factors determine the true effectiveness of a shielding tape when appleid, including type and thickness of foil, adhesive type, closeness of contact, smoothness of application surface, strength and frequency of the EMI signal, etc. Still, an attenuation value can be determined using standard tests and fixtures.

当使用时很多因素决定了一个屏蔽带子的真实效能，包括带子的类型和厚度，黏合剂类型，接触的紧密程度，应用表面的平滑度，EMI信号的强度和频率，等等。虽然如此，使用标准测试和夹具一个衰减值能被确定。

For tape, typical shielding effectiveness (far field) is in the range of 60dB to 80dB (10 KHz to 20 GHz). For more specifications see table.

对于带子，典型的屏蔽效能（远场）是在60dB到80dB (10 KHz到20 GHz)的范围。对于更多的规格请看表。

We can slice all our tapes in any width我们能将所有的带子切成任何宽度。

| 3201 | Technical drawing技术设计图: |
| --- | --- |
| Copper tape with conductive adhesive带有自粘的铜带 A soft metal foil with a higly conductive self-adhesive on one side, with a release liner. 一个软金属薄片在一侧上带有一个高导电自粘，带有一个解开衬套。 Conductive acrylic adhesive 导电丙烯酸黏合剂 Supplied on a removable liner for easy handling and die-cutting供货在一个活动衬套上为了容易操作和冲切。 Like all our shielding system tapes, copper tape 3201 is available in standard and custom widths and lengths. Standard length is 16,5 meter. 像所有我们的屏蔽系统带子一样，铜带3201是可以提供标准的和定制的宽度和长度。标准长度是16.5米。 The tape is standard available in标准供应大带子是: 0.035 mm (part no零件号. 3201) 0,12 mm (part no零件号. 3212) 0,18 mm (part no零件号. 3218) Other on request其它的根据需求 Click here to download the data sheet |  |
| 3202 | Technical drawing技术设计图: |
| Tinned copper tape镀锡铜带 Like tape 3201 with added tin layer for corrosion protection and improved solderability.像带子3201带有附加的锡层用于防腐和改进可焊性。 |  |
| 3203 | Technical drawing技术设计图: |
| Aluminium tape铝带 Developed espacially for aluminium housings and frames to prevent galvanic corrosion.开发特别用于铝机壳和机架以预防电化腐蚀。 |  |
| 3204 | Technical drawing技术设计图: |
| Contact Surface Tape接触面带子 A metal tape with a highly conductive self-adhesive on one side and masking tape on the other side.一个金属带在一侧带有高导电自粘和在另一侧有掩蔽带子。 This contact surface tape is used to improve the corrosion resistance of construction metals (like untreated steel plates), or to improve the galvanic compatibility when 2 metal parts are connected with a gasket. After the parts have been coated, the paint overlaps the metal tape to increase the bonding. 这个接触面带子被用于改进金属结构的耐蚀性（像天然的钢板），或当2个金属部件用垫圈连接时用于去改进电化兼容性。在零件被涂覆后，油漆覆盖金属带以增加连接。 For more specifications see table.更多的应用请看表。 |  |
| 3205 | Technical drawing技术设计图: |
| Mounting tape安装带 A double-sided self-adhesive transfer tape for mounting purposes. This system can be applied much faster than a conductive glue and can be applied very accurately. No time required for curing (pressure sensitive version). For lower resistance and/or to fill gaps with a rough surface we recommand Shieldokit electrical conductive 2 components adhesive. (see conductive glue) 一个双边自粘的转接带用于安装目的。这个系统能比导电胶水应用的更快，而且能被使用的非常精确。对于固化没有时间的要求（压敏感区）。对于更低的阻抗和/或去填满带有粗糙的表面的间隙我们推荐屏蔽套件电传导2部件黏合剂。（看导电胶水） for more specifications see table below更多的规格看下表、 Click here to download the data sheet |  |
| 3206 | Technical drawing技术设计图: |
| Die-cut mounting tape / Sandwich copper tape 冲切安装带/多层铜带 A soft metal foil, laminated on 2 sides with a conductive self-adhesive. This is available in sheets and rolls. 一个软金属薄片，在2边上锻压带有一个导电自粘。这个可获得以薄片和卷的形式。 for more specifications see table below更多的规格看下表 |  |
| 3207 | Technical drawing技术设计图: |
| Copper tape with paper insulation带有纸绝缘的铜带 Same as 3201 but with a paper layer added to insulate the top layer of the copper tape. Thickness of the copper is 0.035 mm with a 0.5 mm thick paper insulation layer. Available in 1500 mm width. 与3201相同，但对于铜带的顶层用一个纸层增加绝缘。铜的厚度是0.035mm，带有一个0.5mm厚度的纸绝缘层。可获得的宽度在1500mm。 |  |
| 3208 | Technical drawing技术设计图: |
| Mu-ferro tape钼-铁氧体带子 Metal tape used for shielding against low magnetic frequency's.金属带用于屏蔽以防低的磁场频率。 |  |
| 4703 | Technical drawing技术设计图: |
| Amucor tape带子 This is a 11 micron thick Amucor tape (Aluminium type), reinforced with 23 micron thick polyester and an acrylic adhesive on the back. 这是一个11微米厚的Amucor带子（铝类型），在背面加固有23微米厚的聚酯纤维和一个丙烯酸黏合剂。 |  |
| 4713 | Technical drawing: |
| Conductive textile tape导电织物带 Nylon ribstop, extreme strong + flexible. Metalized with Cu/Ni with conductive adhesive on the back (See 3205). 尼龙肋骨顶，极其牢固+柔软。用铜/镍金属化在背部带有导电自粘（看3205）。 |  |
| 4718 | Technical drawing技术设计图: |
| Amucor with PET in the middle Amucor在中部带有PET Sandwich tape with 2 layers of 11 micron thick aluminium with 23 micron polyester inside. 多层带带有11微米厚的铝2层，在内侧带有23微米的聚酯纤维。 |  |

Technical specification and part numbers技术规格和零件号

| part nr. 零件号 (Conductive adhesive导电自粘) | 3201 | 3202 | 3203 | 3204 | 3205 | 3206 |
| --- | --- | --- | --- | --- | --- | --- |
| part nr. 零件号 (Standard adhesive标准黏合剂) | 3301 | 3302 | 3303 | 3304 | - | 3306 |
| Construction结构 |  |  |  |  |  |  |
| foil material薄片材料 | soft copper软铜 | soft copper软铜 | Aluminium铝 | soft copper软铜 | Adhesive黏合剂 | soft copper软铜 |
| Surface表面 | Shiny明亮的 | Tinned镀锡的 | Shiny明亮的 | Shiny明亮的 | - | - |
| foil thickness薄片厚度 | 0.035 mm | 0.035 mm | 0.040 mm | 0.035 mm | - | 0.035 mm |
| total thickness 总的厚度 | 0.060 mm | 0.060 mm | 0.065 mm | 0.060 mm | 0.050 mm | 0.085 mm |
| Adhesive黏合剂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 |
| adhesive performance黏合剂性能 | 4.5 N/cm | 4.5 N/cm | 4.5 N/cm | 4.5 N/cm | 4.5 N/cm | 4.5 N/cm |
| tensile strength拉伸强度 | 55 N/cm | 40 N/cm | 25 N/cm | 55 N/cm | - | 55 N/cm |
| temperature resistance耐温性 | 155 °C | 155 °C | 155 °C | 155 °C | 155 °C | 155 °C |
| el. resistance through adhesive 穿过黏合剂的电阻 | 0.003 Ohm | 0.003 Ohm | 0.003 Ohm | 0.003 Ohm | 0.003 Ohm | 0.003 Ohm |
| standard roll widths卷的标准宽度 (mm) | 10, 25, 50, 100 | 10, 25, 50, 100 | 10, 25, 50, 100 | 10, 25, 50, 100 | 10, 25, 50, 100 | 10, 25, 50, 100 |
| roll lengths卷长度 | 16.5 m | 16.5 m | 16.5 m | 16.5 m | 66 m | 16.5 m |

*Other roll length on request其它的卷长度根据需求

| part nr.零件号 (Conductive adhesive导电粘合剂) | 3207 | 3208 | 4703 | 4713 | 4718 |
| --- | --- | --- | --- | --- | --- |
| part nr. 零件号 (Standard adhesive标准粘合剂) | 3307 | 3305 | 4702 | 4712 | 4717 |
| Construction结构 |  |  |  |  |  |
| foil material薄片材料 | soft copper with paper带有纸的软铜 | Mu-ferro钼-铁氧体 | Amucor | Conductive textile导电织物 | Amucor and PET |
| Surface表面 | Bright明亮的 | Tinned镀锡的 | Bright明亮的 | Textile织物 | Bright明亮的 |
| foil thickness薄片厚度 | 0.035 mm | 0.1 mm | 0.023 mm | 0.06 mm | 0.35 mm |
| total thickness 总的厚度 | 0.060 mm | 0.125 mm | 0.048 mm | 0.0825 mm | 0.3725 mm |
| Adhesive黏合剂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 | synthetic conductive resin合成导电树脂 |
| adhesive performance黏合剂性能 | 4.5 N/cm | 4.5 N/cm | 4.5 N/cm | 4.5 N/cm | 4.5 N/cm |
| tensile strength拉伸强度 | 55 N/cm | - | - | - | - |
| temperature resistance 耐温性 | - | - | - | - | - |
| el. resistance through adhesive 穿过黏合剂的电阻 | 0.003 Ohm | 0.003 Ohm | 0.003 Ohm | 0.003 Ohm | 0.003 Ohm |
| standard roll widths标准卷宽度 (mm) | 10, 25, 50, 100 | 10, 25, 50, 100 | 10, 25, 50, 100 | 10, 25, 50, 100 | 10, 25, 50, 100 |
| roll lengths卷长度 | 16.5 m | 16.5 m | 16.5 m | 66 m | 16.5 m |

*Other roll length on request其它的卷长度根据需求

Example举例

Copper tape with conductive adhesive (3201) 25 mm wide and 16.5 meters long. Order code: 3201-25-16.5

带有导电黏合剂的铜带（3201） 25mm宽和16.5米长。订购号：3201-25-16.5

| Part number零件号 | Width宽度 (mm) | Length长度 |
| --- | --- | --- |
| 3201 | 25 | 16.5 |
| For part numbers see table above零件号看上表 |  |  |